SECTION 06600

Glass Fiber Reinforced Stone

- GENERAL

  - SECTION INCLUDES

    - Glass fiber reinforced stone fabrications as indicated on the drawings.

  - RELATED SECTIONS

    - Section 04720 - Cast Stone.

    - Section 05500 - Metal Fabrications:  Supplementary supports for large items.

    - Section 06100 - Rough Carpentry:  Supplementary supports for large items.

    - Section 06610 - Glass Fiber Reinforced Plastic Fabrications.

    - Section 09235 - Glass Fiber Reinforced Gypsum Fabrications.

    - Section 09900 - Paints and Coatings:  Field painting and sealing prior to painting.

  - REFERENCES

    - ASTM C 150 - Standard Specification for Portland Cement; 1999a.

    - ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials; 1999.

    - ASTM G 23 - Standard Practice for Operating Light-Exposure Apparatus (Carbon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials; 1996.

  - SUBMITTALS

    - Submit under provisions of Section 01300.

    - Product Data:  Manufacturer's data sheets on each product to be used, including dimensions, finishes, storage and handling requirements and recommendations, and installation recommendations.

    - Shop Drawings:  For custom items, provide drawings showing dimensions, layout, joints, details, and interface with adjacent work; include field measured dimensions of the spaces where items are to be installed, if critical to proper installation.

    - Samples:  For each custom finish specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.

  - QUALITY ASSURANCE

    - Installer Qualifications:  Regularly engaged and experienced in the installation of glass fiber reinforced stone units.

  - DELIVERY, STORAGE, AND HANDLING

    - Transport, lift, and handle units with care, avoiding excessive stress and preventing damage; use appropriate equipment.

    - Store products in manufacturer's unopened packaging until ready for installation, in a clean dry area protected from weather, moisture and damage; store units upright and not stacked unless permitted by manufacturer.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer:  Stromberg Architectural Products Inc; PO Box 8036, I-30 West, 4400 Oneal, Greenville, TX  75404. ASD.  Tel: (903) 454-0904.  Fax: (903) 454-3642.  Email: sales@strombergarchitectural.com.   www.strombergarchitectural.com.

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - MATERIALS

    - Glass Fiber Reinforced Stone Fabrications:  High density polymer, crushed stone and/or silica sand, reinforced with chopped glass fiber mat and structural reinforcing as required.

      - Color:  As selected from manufacturer's selection.

      - Color:  To match Architect's sample.

      - Shell Thickness:  1/8 to 1/2 inch, nominal.

      - Surface Burning Characteristics:  Flame spread index of less than 25 (class A), smoke developed index of less than 450, when tested in accordance with ASTM E 84.

      - Flexural Strength:  20000 psi (138 MPa), when tested in accordance with ASTM D 790.

      - Modulus of Elasticity:  0.9 x 10^6 psi (6200 MPa), when tested in accordance with ASTM D 790.

      - Tensile Strength:  12000 psi (83 MPa), when tested in accordance with ASTM D 638.

      - Compressive Strength:  17000 psi (117 MPa), when tested in accordance with ASTM D 695.

      - Bearing Strength:  9000 psi (62 MPa), when tested in accordance with ASTM D 638.

      - Thermal Expansion Coefficient:  10 x 10^-6 per degree F (5.56 x 10^-6 per degree C).

      - Specific Gravity:  1.5.

      - Variation in Thickness From Nominal:  Minus 1/16 inch (1.5 mm), plus 1/4 inch (6 mm).

      - Variation from Dimensions Indicated on Drawings:  Plus and minus 1/8 inch (3 mm), maximum.

      - Variation from Square:  Plus and minus 1/4 inch (3 mm), maximum.

      - Variation of Hardware From Intended Location:  Plus and minus 1/4 inch (6 mm), maximum.

      - Provide concealed reinforced anchorage points for anchors of type recommended by manufacturer.

      - Mark each unit with permanent serial number coordinated with shop drawing designators.

      - Cure and clean prior to shipment; remove material that may be toxic to plant or animal life or incompatible with adjacent building materials.

      - Outside Corner Radius:  1/16 inch to 1/8 inch (1.5 to 3 mm).

      - Draft Angle:  3 degrees, minimum, on returns, setbacks, reveals, and grooves.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed; verify that substrates are plumb and true.

    - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

    - Check field dimensions before beginning installation.  If dimensions vary too much from design dimensions for proper installation, notify Architect and wait for instructions before beginning installation.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

    - Install supplementary temporary and permanent supports as required for proper installation.

  - INSTALLATION

    - Install in accordance with applicable code and manufacturer's recommendations, plumb and true to line; shim where necessary.

    - Provide control joints at not more than 35 feet (10.5 m) on center if not indicated on drawings.

    - Provide expansion joints where moving joints in substrate occur.

    - Patch exposed anchor points to match color and texture of unit.

  - PROTECTION

    - Protect installed products until completion of project.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION