SECTION 02815

Glass Fiber Reinforced Concrete Tables and Stools

- GENERAL

  - SECTION INCLUDES

    - Glass fiber reinforced concrete tables and stools as indicated on the drawings.

  - RELATED SECTIONS

    - Division 04 Section “Cast Stone”.

    - Division 05 Section “Metal Fabrications” for supplementary supports for large items.

    - Division 06100 Section “Rough Carpentry” for supplementary supports for large items.

- Division 06610 Section “Glass Fiber Reinforced Plastic Fabrications”.

- Division 09235 Section “Glass Fiber Reinforced Gypsum Fabrications”.

- Division 09900 Section “Paints and Coatings” for field painting and sealing prior to painting.

  - REFERENCES

- ASTM C 150 - Standard Specification for Portland Cement; 1999a.

- ASTM C 33-99 Concrete Aggregates

- ASTM C 666 – Standard test Method for Resistance of Concrete to Rapid Freezing and Thawing

- ASTM C 979-82(1993):  Pigments for Integrally colored Concrete.

- ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials; 1999.

- ASTM G 23 - Standard Practice for Operating Light-Exposure Apparatus (Carbon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials; 1996.

  - SUBMITTALS

    - Submit under provisions of Section 01300.

    - Product Data:  Manufacturer's data sheets on each product to be used, including dimensions, finishes, storage and handling requirements and recommendations, and installation recommendations.

    - Shop Drawings:  For custom items, provide drawings showing dimensions, layout, joints, details, and interface with adjacent work; include field measured dimensions of the spaces where items are to be installed, if critical to proper installation.

    - Samples:  For each custom finish specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.

  - QUALITY ASSURANCE

    - Manufacturer: Obtain GFRC table(s) as manufactured by a firm specializing in the manufacture of GFRC table(s), with a minimum of ten years experience.

    - Provide a list of projects comparable in size, scope, and complexity as indicated.

    - Provide verification that glass fiber reinforced concrete table meets or exceeds products specified.

    - Installer Qualifications:  Regularly engaged and experienced in the installation of glass fiber reinforced concrete products.

  - DELIVERY, STORAGE, AND HANDLING

- Transport, lift, and handle units with care, avoiding excessive stress and preventing damage; use appropriate equipment.

- Store products in manufacturer's unopened packaging until ready for installation, in a clean dry area protected from weather, moisture and damage; store units upright and not stacked unless permitted by manufacturer.  Product shall be stored clear of the ground on non-staining pallets or other temporary planking.

- Protect product from staining, chipping, and other damage.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer:  Stromberg Architectural Products Inc; PO Box 8036, I-30 West, 4400 Oneal, Greenville, TX  75404. ASD.  Tel: (903) 454-0904.  Fax: (903) 454-3642.  Email: sales@strombergarchitectural.com.   www.strombergarchitectural.com.

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - MATERIALS

    - Glass Fiber Reinforced Concrete Tables and Stools:  High density concrete made of ASTM C 150 Portland cement, crushed stone, silica sand, and polymers reinforced with glass fiber and structural reinforcing as required; asbestos free.

      - Color:  As selected from manufacturer's selection.

- Color:  To match Architect's sample.

- Surface Texture:  Exposed surface as selected from manufacturer’s selection

- Style:  (Select One) [Manufacturer’s model number [T_S_2_36_R] [T_S_2_36_S] [T_S_2_60_R] [T_S_2_60_S]] [As indicated in drawings.]

- (If indicated on drawings, use paragraphs below)

  - Table Dimensions:  (Select One) [__ft. __in. Square] [___ft. ___in. Radius] [As indicated on drawings.]

  - Stool Dimensions:  #  stools; (Select One) [__ft. __in. Square] [___ft. ___in. Radius] [As indicated on drawings.]

  - Table Height:  [___ft. ___in.] [As indicated on drawings.]

  - Stool Height:  #  stools [___ft. ___in.] [As indicated on drawings.]

- Density:  140 pcf (2240 kg/cu m).

- Shell Thickness:  3/8” to 3/4 inch (9.5 mm), nominal.

- Surface Burning Characteristics:  Flame spread index of 0, smoke developed index of 5; when tested in accordance with ASTM E 84.  Fuel contribution of 3.

- Weather Resistance:  No significant loss in strength or change in appearance after 200 hours accelerated weathering conducted in accordance with ASTM G 23.

- Flexural Strength:  1000 to 1800 psi (6.9 to 12.4 MPa).

- Modulus of Elasticity:  2 x 10^5 psi (1370 MPa).

- Compressive Strength:  Over 5000 psi (34 MPa).

- Variation from Dimensions Indicated on Drawings:  Plus and minus 1/8 inch (3 mm), maximum.

- Variation from Plane Along Edge or Surface:  Plus and minus 1/16 inch per linear foot (1.5 mm in 300 mm), maximum.

- Outside Corner Radius:  1/16 inch to 1/8 inch (1.5 to 3 mm).

- Draft Angle:  3 degrees, minimum, on returns, setbacks, reveals, and grooves.

- Provide non-corrosive screwed or bolted anchors with reinforced holes through face of units.

- Provide non-corrosive anchors and reinforced anchoring points as indicated on drawings.

  - Exposed Anchors: Type 304 Stainless Steel unless otherwise indicated.

  - Concealed Anchors:  Hot-dipped Galvanized Steel unless otherwise indicated.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed; verify that substrates are plumb and true.

    - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

      - Proceed with installation only after unsatisfactory conditions have been corrected.

    - Check field dimensions before beginning installation.  If dimensions vary too much from design dimensions for proper installation, notify Architect and wait for instructions before beginning installation.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with applicable code and manufacturer's recommendations, plumb and true to line; shim where necessary.

    - Patch exposed anchor points to match color and texture of unit.

- Clean GFRC units according to manufacturer’s written instructions.

      - Remove dirt, stains, or other residue.

      - Protect surrounding materials and surfaces during cleaning.

  - PROTECTION

    - Protect installed products until completion of project.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION